## Slide 1: Measurement techniques for energy rating of PV modules at TÜV Rheinland PV test laboratories 7th Energy Rating and Module Performance Modelling Workshop 30/31 March 2017, Lugano, Switzerland Werner Herrmann, Markus Schweiger TÜV Rheinland Energy GmbH

## Slide 2: Introduction
30.03.2017
2
7th Energy Rating and Module Performance Modelling Workshop 30/31 March 2017, Lugano, Switzerland
Assessment of the PV module energy yield performance requires knowledge of specific module parameters
Measurement procedures are defined in IEC 61853-1 and IEC 61853-2
TÜV Rheinland operates five energy yield test sites and has more than 10 years experience in energy yield testing of PV modules

## Slide 3: Output power under variable temperature and irradiation Test equipment
30.03.2017
3
7th Energy Rating and Module Performance Modelling Workshop 30/31 March 2017, Lugano, Switzerland
Pulsed solar simulator: Pasan SunSim 3b (Multiflash / Dragon-back technique, spectrally neutral attenuation masks)
              Berger Lichttechnik PSS30 (Separable test chamber for temperature conditioning of the PV module)
Steady state solar simulator: Customized set-up with 12 metal halide lamps (Reduction of thermal radiation, temperature conditioning of the PV module under illumination)
Pulsed solar simulator
Steady state solar simulator

## Slide 4: Output power under variable temperature and irradiation PV Module I-V correction parameters (IEC 60891)
30.03.2017
4
7th Energy Rating and Module Performance Modelling Workshop 30/31 March 2017, Lugano, Switzerland
Legend:
I1, I2: Module current
V1, V2: Module voltage
T1, T2: Module temperature
G1, G2: Irradiance
Index 1: Measurement conditions
Index 2: Target conditions (i.e. STC)
Module parameters:
rel : Temperature coefficient ISC [1/K]
rel : Temperature coefficient VOC [1/K]
RS’: Internal series resistance []
’ : Temperature coefficient RS [/K]
a: Irradiance correction factor of VOC
Note:
Temperature coefficients are typically related to STC
Two options to cover the range of test conditions:
Measurement of performance matrix in accordance with IEC 61853-1
I-V reference curve + Determination of I-V correction parameters in accordance with IEC 60891
IEC 60891
Procedure 2

## Slide 5: Output power under variable temperature and irradiation Determination of I-V correction parameters (IEC 60891)
30.03.2017
5
7th Energy Rating and Module Performance Modelling Workshop 30/31 March 2017, Lugano, Switzerland
Matrix measurements
@ 25°C, 450 – 1000 W/m²
Module I-V correction parameters
(Module type: multi c-Si, 60 cells)
α REL = -0.042% K-1 RS’ = 460 mOhm
β REL = -0.46% K-1 a = 0.054
‘ = -0.004% K-1
Translated I-V curves at STC
Note:
I-V correction parameters may be subject to production tolerances
IEC 60891 Parameter
Optimierung
Matrix measurements
@ 1000 W/m², 25 – 65°C
Variable temperature
Variable irradiance

## Slide 6: Output power under variable temperature and irradiation Spread of I-V correction parameters
30.03.2017
6
7th Energy Rating and Module Performance Modelling Workshop 30/31 March 2017, Lugano, Switzerland

## Slide 7: Output power under variable temperature and irradiation Low irradiance behavior of different PV modules
!
30.03.2017
7
7th Energy Rating and Module Performance Modelling Workshop 30/31 March 2017, Lugano, Switzerland
References:
M. Schweiger et al.: Understanding the energy yield of photovoltaic modules in different climates by linear performance loss analysis of the module performance ratio, IET Renewable Power Generation, ISSN 1752-1416, 2017
Schweiger et al.: Performance Stability of Photovoltaic Modules in Different Climates, Paper submitted to Progress in PV
Drop of module efficiency in the low irradiance range <200 W/m²
c-Si PV technologies: -2% to -4%
CIGS thin-film: -5% to -10%
CdTe thin-film: 0% to -3%
a-Si thin-film: -2% to -8%
PV module performance under variable irradiation is important for locations with high low irradiance contribution to annual insolated solar radiation (i.e. Cologne: 19%)
No generalization possible

## Slide 8
30.03.2017
8
7th Energy Rating and Module Performance Modelling Workshop 30/31 March 2017, Lugano, Switzerland
Test program:
3 Test samples
x 23 Test conditions
x 3 I-V measurements
207 I-V measurements
Output power under variable temperature and irradiation Improvement of IEC 61853-1
Cologne
Saudi-Arabia
Number of test conditions shall be reduced:
  Temperature coefficients at 200 /1000 W/m²
  Variable irradiation at 25°C
  Other data points can be extrapolated (IEC 60891)

## Slide 9: Spectral response Spectral response measurement (IEC 60904-8)
30.03.2017
9
7th Energy Rating and Module Performance Modelling Workshop 30/31 March 2017, Lugano, Switzerland
References:
Y. Hishikawa et al.: Spectral response measurements of PV modules and multi-junction devices, 22nd EU PVSEC, 2007
Y. Tsuno et al.: A method for spectral response measurements of various PV modules, 23rd EU PVSEC, 2008
Test equipment:
High resolution monochromator, Model: Bunkoh-Keiki CEP-M77
Features:
Non-destructive measurement of full-size PV module
Measurement procedures for crystalline silicon and thin-film PV modules
White and color bias light: Single junction and multi junction measurements
Measurement of SR non-uniformity in the active module area
Technical data: | 
Monochromatic light: | 50 mm x 50 mm
Wavelength range: | 300 – 1700 nm
Wavelength interval: | 1, 5, 10, 50 nm
Max. module dimension: | 200 cm

## Slide 10: Spectral response Spread of SR curves for different PV technologies
30.03.2017
10
7th Energy Rating and Module Performance Modelling Workshop 30/31 March 2017, Lugano, Switzerland
Spread of SR curves is observed for all PV technologies
Future advances in cell technology will increase the spread

## Slide 11: Angular response Concepts for angular response measurement on cell level
30.03.2017
11
7th Energy Rating and Module Performance Modelling Workshop 30/31 March 2017, Lugano, Switzerland
Manufacture of a mini-module:
Identical optical construction compared to PV module
Test cell = center cell
Destructive test method:
PV module
Test cell is electrically contacted through backsheet
TUV non-destructive test method:
PV module
Isc of test cell is concluded from PV module I-V curve under partially shading

## Slide 12: Angular response Non-destructive angular response measurement
30.03.2017
12
7th Energy Rating and Module Performance Modelling Workshop 30/31 March 2017, Lugano, Switzerland
Measurements for each AoI setting:
I-V curve of fully irradiated PV module with N cells  (I-V)N
I-V curve of PV module with test cell 50% partially shaded  (I-V)50%
Isc of test cell:
2.83 A
– I-V curve (I-V)N : Non-shaded, N cells
– I-V curve (I-V)N-1 : Non-shaded, (N-1) cells
– I-V curve (I-V)50% : Test cell 50% shaded
Calculations for each AoI setting:
PV module I-V curve of (N-1) solar cells  (I-V)N-1
Intercept point between I-V curves (I-V)N-1 and (I-V)50%  Isc of test cell
Reference:
W. Herrmann et al.: Solar simulator measurement procedures for determination of the angular characteristic of PV modules, 29th EU PVSEC, Amsterdam, 2014
Note:
Steps in I-V curves originate from non-uniform illumination of the PV module when rotating around the vertical axis through the module center.

## Slide 13: Angular response Non-destructive angular response measurement
30.03.2017
13
7th Energy Rating and Module Performance Modelling Workshop 30/31 March 2017, Lugano, Switzerland
Angular response (AR) curve /Incident angle modifier (IAM)
c-Si PV module

## Slide 14: Angular response Angular response range of different glass types
30.03.2017
14
7th Energy Rating and Module Performance Modelling Workshop 30/31 March 2017, Lugano, Switzerland
Modelling of angular response curve (IEC 61853-2):
Good fit in the angular range < 80° (RSME <1%)
Standard float glass (SFG): ar = 0.159
AR coated glass (ARC): ar = 0.144
Type | ar
SFG1 | 0.167
SFG2 | 0.154
SFG3 | 0.166
SFG4 | 0.165
SFG5 | 0.159
SFG6 | 0.155
SFG7 | 0.153
SFG8 | 0.149
SFG9 | 0.157
SFG10 | 0.163
SFG11 | 0.155
Average | 0.159
Type | ar
ARC1 | 0.151
ARC2 | 0.133
ARC3 | 0.164
ARC4 | 0.163
ARC5 | 0.133
ARC6 | 0.139
ARC7 | 0.142
ARC8 | 0.141
Average | 0.144
Standard float glass (SFG)
AR coted glass (ARC)
References:
W. Herrmann et al.: Optical characteristics of PV module front glasses – Incidence angle effects of various glass types and impact on annual energy yield, 28th EU PVSEC, Paris, 2013
N. Martin et al.: Calculation of the PV modules angular losses under field conditions by means of an analytical model, Solar Energy Materials & Solar Cells 70 (2001) 25-38

## Slide 15: Nominal module operating temperature IEC 61853-2 procedure
30.03.2017
15
7th Energy Rating and Module Performance Modelling Workshop 30/31 March 2017, Lugano, Switzerland
u0  Impact of solar irradiance
u1  Impact of wind speed (WS)
Modelling of module operating temperature:
Problems:
Required wind speed interval of 4 m/s is too large for urban test locations
 Reduce minimum WS interval to 3 m/s
Data filtering still results in large scattering of accepted data points
 Wind direction should be considered
Note:
Coefficients are dependent on installation conditions and test location
!
Data filtering  No valid data set for Cologne since March 2016!
Required WS interval

## Slide 16: Conclusions
30.03.2017
16
7th Energy Rating and Module Performance Modelling Workshop 30/31 March 2017, Lugano, Switzerland
Within all PV technologies (thin-film and c-Si) significant scattering of energy yield performance was observed
Individual performance characterization of a module type is required
Data sheet information of PV modules does not cover the needs for energy rating
Test requirements of IEC 61853-1 and IEC 61853-2 shall be improved to perform measurements with reasonable constrains of costs and time
IEC 60891 shall be applied to reduce test work in the laboratory

## Slide 17
Thank you for your attention!
Dr. Werner Herrmann
TÜV Rheinland Energy GmbH
werner.herrmann@de.tuv.com http://www.tuv.com/solarpower
7th Energy Rating and Module Performance Modelling Workshop 30/31 March 2017, Lugano, Switzerland